## Slide 2: Phosphorene and 2D materials
J. Brndiar, Y. Huang, A. Faizan, Marko Milivojevic,
I. Štich
CCMS, Inst. of Physics, Slovak Academy of Sciences
SLOVAK ACADEMY OF SCIENCES
Funding:
http://www.fu.sav.sk

## Slide 3: Phosphorene and 2D materials
J. Brndiar1, Y. Huang1, A. Faizan1, Marko Milivojevic,
T. Frank2, R. Derian1, K. Tokár1, L. Mitas3, J. Fabian2, I. Štich1
1 CCMS, Inst. of Physics, Slovak Academy of Sciences, Bratislava, Slovakia
2 University of Regensburg, Inst. for Theoretical Physics, Germany
3 Dept. of Physics, North Carolina State University, Raleigh, U.S.A.
http://www.fu.sav.sk
Funding:

## Slide 4: Outline:
Intro. 2D materials and phosphorene
Summary
Calculations: 1) completed, phosphorene
- band gap
- cohesion
2) in progress, phosphorene
- strain effects
3) in preparation, MoS2
- strain effects
- vdW multilayers

## Slide 5: 2D materials
a number of 2D materials prepared by:
- exfoliation (gr, phosphorene, TM -dichalcogenides)
- epitaxial growth (silicene, germanene…)
electronic properties:
metals  semimetal  semiconductor  wide gap insulator
Pd, Rh
graphene
TMD
h-BN
high carrier mobility
high-mobility high-speed and fast switching semiconductor devices requiring low D-materials
direct band gap (often)

## Slide 6: 2D materials
2D materials: bandgaps
exciton
trion
gap states
fundamental (quasiparticle) gap
optical gap
fundamental (quasiparticle) gap:
f
exciton
excitonic binding energy:
e
optical gap:
o = f - e 
universal scaling relation (in 2D) for e:
e = f / 4
Z. Jiang, Z. Liu, Y. Li, and W. Duan, Phys. Rev. Lett. 118, 266401 (2017)
DFT, GW
BSE…GW-BSE
difficult
easy

## Slide 7: 2D material phosphorene
What did we learn from 2D phosphorene???
Calculations: 1) previous, phosphorene
- band gap
- cohesion

## Slide 8: 2D material phosphorene
band gaps:

## Slide 9: 2D material phosphorene
band gaps:

## Slide 10: 2D material phosphorene
band gaps:
!!!o reflects genuine exp. spread!!!
need for much more accurate methods than
DFT, GW, GW-BSE !!!
QMC
 typical also for other 2D materials

## Slide 11: QMC: calculations
3 complete QMC calculations (including finite-size scaling):
periodic setup: 11… 66 i.e. 20…720 explicitly corr. electrons
- B3LYP nodal hypersurfaces
- PBE nodal hypersurfaces
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).

## Slide 12: QMC: calculations
3 complete QMC calculations (including finite-size scaling):
periodic setup: 11… 66 i.e. 20…720 explicitly corr. electrons
- B3LYP nodal hypersurfaces
- PBE nodal hypersurfaces
cluster setup: 44, 55, 66
- B3LYP nodal hypersurfaces
strict upper bound
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).

## Slide 13: QMC electronic band gap
extrapolation to N   :
thermodynamic limit
linear in 1/N
(N = 4  L  L)
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).

## Slide 14: QMC electronic band gap
DFT
1eV
GW
1eV
exp.
1eV
DMC: f  2.4 eV
PBE/DMC, PBC
B3LYP/DMC, clust.
DMC
0.2 eV
e  0.6 eV
o  1.8 eV
B3LYP/DMC, PBC
GW: underestimates f
f  2.4 eV
e  0.65 eV
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).
L. Li, J. Kim, C. Jin, et al. Nat. Nanotechnol. 12, 21 (2016).

## Slide 15: QMC electronic band gap
DFT
1eV
GW
1eV
exp.
1eV
DMC: f  2.4 eV
DMC
0.2 eV
e  0.6 eV
o  1.8 eV
f  2.3-2.4 eV
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).
X.Wang, A. M. Jones, K. L. Seyler, et al.,Nat. Nanotechnol. 10, 517 (2015).

## Slide 16: QMC cohesion
L. Shulenburger, A. D. Baczewski, Z. Zhu, J. Guan, and D. Tománek, Nano Lett. 15, 8170 (2015).
- 3D crystal: 3:43 eV/atom (expt.)
- interlayer binding: 816 meV/atom (QMC calc.)
Ch. Kittel, Introduction to Solid State Physics, 8th ed. (John Wiley & Sons, Inc., NJ, 2005) p. 50.
thermodynamic path:
P4 molecule bulk black phosphorus phosphorene
fixed node error correction:
P atom and P4 molecule
(CCSD(T) in CBS limit):
0.09 eV/atom B3LYP/DMC
0.09 eV/atom PBE/DMC
3.284(6) eV/atom B3LYP/DMC
3.268(4) eV/atom PBE/DMC
 ground-state essentially exact
T. Frank, R. Derian, K. Tokár, L. Mitas, J. Fabian, and I. Štich, Phys. Rev. X 9, 011018 (2019).

## Slide 17: 2D materials tuning
c
2D materials can be tuned by:
- # of layers
- # applied strain:
MoS2: strainability: >10%, gap: <0,1.8> eV
- dielectric environments:
substrates
capping

## Slide 18: 2D materials tuning
2D materials can be tuned by:
- proximity effects
semiconductor +
carrier mob.
strong spin effects 
- manipulate directly
spin-orbit coupling
manipulation of spin prop. via orbital prop.


## Slide 19: 2D materials strain
Calculations: 2) in progress, phosphorene
- strain effects

## Slide 20: Strain in 2D phosphorene
quasiparticle band gap scales linearly with the applied strain (see dashed lines which highlight the gap ratios for -1.00%: 0%: 2.5% ).
highly nontrivial as the band gaps are differences between ground- and excited-state PESs.
The strain band gap tuning is quite strong; the QMC values are about factor 2 stronger than those resulting from DFT (PBE, B3LYP) treatment, not shown.
Eg [eV]
44
55
66
!!!However, we don‘t know the unstrained structure!!!
(lattice parameters a and b taken from 3D black phosphorus crystal)
...and internal parameters y and z only DFT optimized
more serious
less serious
4 structural parameters
J. Brndiar, L. Mitas, J. Fabian, and I. Štich, in preparation (2021)

## Slide 21: Strain in 2D phosphorene
Full approach:
fixing all 4 parameters a, b, y, and z: paraboloid approximation
this allows calculation of the effect of arbitrary strains:
- uniaxial
- biaxial

fitted analytical formula for
ground- and excited states

previous results
3D crystal

 large modification of the b lattice parameter
to fit the 4 structural parameters, a
grid of 25 points around the
presumed minimum was selected
total ground-state energies calculated
4D paraboloids were fitted taking
into account the QMC error bars.
 more modest modification of the other 3 parameters
J. Brndiar, L. Mitas, J. Fabian, and I. Štich, in preparation (2021)

## Slide 22: 2D material MoS2
8x4
a [Å]
b [Å]
y [Å]
z [Å]

## Slide 23: 2D material MoS2
8+8: twist average
a [Å]
b [Å]
y [Å]
z [Å]

## Slide 24: 2D material MoS2
tuning structural & electronic properties of MoS2:
R. Ganatra and Q. Zhang, ACS Nano 8, 4074 (2014).
# layers

strain

dielectric embedding

complication (with respect to phosphorene):
- 1-layer direct KK band gap
- 2-layer indirect K/2 band gap

## Slide 25: 2D material MoS2
3) in preparation, MoS2
- strain effects
- vdW multilayers

## Slide 26: 2D materials MoS2
tuning structural & electronic properties of MoS2:
- 1-layer direct KK band gap
cell | 33 | 44 (c) | 55 (c) | 66 | 2323 | 3333 | 4343
# electrons | 234 | 416 | 650 | 936 | 312 | 702 | 1248
- 2-layer indirect K/2 band gap
cell | red | orange | green | blue | black
# electrons | 624 | 936 | 1248 | 1560 | 1872

## Slide 27: ...last but not least...
CPU/GPU hours:
2) Snellius (NL): PRACE Tier 1
3) Summit (ORNL): director award
4) ??? Marconi (IT): PRACE Tier 0??? (with Sandro & Michele)
1) Mare Nostrum: PRACE Tier 0

## Slide 28: Summary
important material characteristics in single layer phosphorene calculated/estimated by QMC:
- fundamental gap f
- optical gap o
- exciton binding energy e
- cohesion
1) previous, phosphorene
2) in progress, phosphorene
effects of strain calculated in single layer phosphorene
- strain effect appears to be massive and quantitatively different from DFT
- fixed-node DMC equilibrium structure found
- b lattice parameter significantly different from the crystal
- calculations will allow to determine the effect of arbitrary strain on the gap
3) in preparation, MoS2
outlooks towards QMC calculation of lazer & train effects in MoS2